## Slide 1: Crystal Ready for Shipment
October 12, 2023
1
A. Liu, B. Liu, A. Somov, V. Berdnikov, H. Voskanyan, A. Asaturyan

## Slide 2: Unpolished-1
All Faces Unpolished
Chips inside
2

## Slide 3: Unpolished-2
All Faces Unpolished
Chips inside
3

## Slide 4: Unpolished-3
All Faces Unpolished
Chips inside
4

## Slide 5: Unpolished-4
All Faces Unpolished
Chips inside and on chamfers
5

## Slide 6
Big chips on faces
Scratch
No. 401
6

## Slide 7: No. 402
Too many chips on chamfers
7

## Slide 8: No. 407
Too many chips on chamfers
8

## Slide 9: No. 417
Too many chips on chamfers
Scratches on faces
Big chamfers

## Slide 10: No. 419
Too many chips on chamfers
Scratches on faces
10

## Slide 11: No. 428
Cloudy Region Inside
11

## Slide 12: No. 443
Cloudy Layer Inside
12

## Slide 13
13
Final Look