## Slide 1: Crystal Quality Test (70 crystals recently received from SICCAS)
A. Somov, V. Berdnikov, H. Voskanyan, A. Asaturyan, A. Liu, B. Liu
September 22, 2023
1

## Slide 2
Overview
19 problematic crystals in total
11 of them shown here
Main problems
- unpolished faces
- big chips inside the crystals
- big chips on face
- too many chips on chamfers
- cloudy region inside
- big chamfers & scratches on face
2

## Slide 3: Unpolished-1
All Faces Unpolished
Chips inside
3

## Slide 4: Unpolished-2
All Faces Unpolished
Chips inside
4

## Slide 5: Unpolished-3
All Faces Unpolished
Chips inside
5

## Slide 6: Unpolished-4
All Faces Unpolished
Chips inside and on chamfers
6

## Slide 7
Big chips (~ 5 mm) on faces
Scratch
No. 401
7

## Slide 8: No. 407
Too many chips on chamfers
(more than 30)
8

## Slide 9: No. 402
Too many chips on chamfers
(the same as in 407)
9

## Slide 10: No. 417
Too many chips on chamfers
Scratches on faces
Big chamfers
10

## Slide 11: No. 419
Too many chips on chamfers
Scratches on faces
11

## Slide 12: No. 428
Cloudy Region Inside
12

## Slide 13: No. 443
Cloudy Layers Inside
13